## Slide 1
Mechanical activation is the enhancement of chemical reactivity of a solid through mechanical treatment without changing its overall composition. The material becomes more susceptible to further chemical transformation or interaction.
Key features:
Non-chemical energy input (mechanical)
Increase in specific surface area and defect density
Improved accessibility of reactive sites
Typically reversible over time if not immediately consumed
Activated state is metastable—materials can relax or age, losing some reactivity if stored.

## Slide 2
Three Types of Mechanical Activation
Structural activation: Physical changes dominate. Particle size reduction, increased surface roughness, higher defect concentration, but minimal chemical transformation. Lattice parameters may shift slightly due to strain.
Chemical activation: Partial breaking of chemical bonds occurs, generating reactive intermediates or dangling bonds. The surface becomes chemically different—presence of radicals, unsaturated sites, or new functional groups.
Reaction activation: The activated material immediately undergoes spontaneous reaction with the surrounding atmosphere (oxygen, moisture) or self-reacts (decomposition). Reactivity is so high that chemical change is ongoing.
Distinction: structural activation → potential for reaction; chemical activation → signs of reaction; reaction activation → observable reaction in progress.

## Slide 3
Characteristics and Effects
Structural effects:
Particle size: 10–100 μm → 100 nm–1 μm range
Specific surface area: increases by 10–100×
Crystallite size: measured by XRD line broadening, often 10–100 nm after milling
Lattice strain: residual stress, microstrains visible in XRD peak broadening
Chemical effects:
Surface composition changes (oxidation, contamination from milling media)
Amorphous layer formation on particle surfaces
Hydration or chemisorption of water/CO₂
Generation of vacancies, dislocations, stacking faults
Property changes:
Density reduction (apparent density due to porosity)
Color changes (oxidation, phase transitions)
Magnetic properties shift (grain size effects)
Solubility and reactivity can increase dramatically

## Slide 4
Factors Controlling Activation
Milling time: Activation increases with time but typically saturates after 10–30 minutes depending on material and equipment. Over-milling can lead to agglomeration or unwanted side reactions.
Milling intensity: Ball size, rotation speed, and impact energy determine how much energy is delivered per unit time. Higher intensity = faster activation.
Nature of material: Hard, brittle materials activate more readily than soft, ductile ones. Crystal structure matters—some phases are more stable against milling.
Atmosphere: Inert vs. air vs. oxygen affects oxidation state, surface reactivity, and product distribution. Water vapor can promote hydration.
Temperature control: Milling generates local heat. For thermally sensitive materials, cooling or short milling bursts are needed to prevent unwanted phase transitions or sintering.
Milling media: Ball material (steel, ceramic, agate) can contaminate the sample or catalyze side reactions.

## Slide 5
Assessment and Characterization
Physical methods:
XRD: peak broadening reveals crystallite size and microstrain (using Scherrer equation, Warren–Averbach analysis)
SEM/TEM: direct observation of particle morphology, surface roughness, layering
BET: nitrogen sorption measures specific surface area
Particle size analysis: laser diffraction or dynamic light scattering
Chemical reactivity tests:
Dissolution kinetics: rate of acid/base dissolution correlates with activation state
Calorimetry (DSC/TGA): exothermic peaks show energy release, thermal stability changes
Reaction onset temperature: compare conventional vs. mechanically activated samples—activated materials react at lower T
Isothermal reaction rate: track conversion over time
Combining methods: Use XRD + DSC + reactivity testing for a complete picture of activation level.

## Slide 6
Applications and Relevance
Mechanical activation is applied before mechanochemical synthesis to:
Increase reaction rate and reduce synthesis time
Lower reaction temperature (energy savings, less side reactions)
Enable reactions that don't proceed without activation
Produce novel metastable phases or nanostructures
Improve mixing and contact between solid reactants
Examples: cement activation for faster setting, metal oxide synthesis at room temperature, polymer crosslinking without initiators.