## Slide 1
MECHANOCHEMICAL SYNTHESIS OF NANOMATERIALS
Advantages for Nanomaterial Production
Mechanochemistry is exceptionally well-suited for synthesizing nanomaterials because it naturally generates nanostructures and offers excellent control:
Particle size control:
Direct relationship between milling energy, time, and final particle size
Predictable size reduction following power-law kinetics
Fine-tuning possible through milling parameters
Scalability:
Processes readily scale from lab (grams) to production (tons)
Same equipment types used across scales; recipes are reproducible
Preventing agglomeration:
Immediate product separation from milling media
Short residence times in hot zones compared to thermal synthesis
Mechanical stirring during synthesis can prevent coalescence
Phase purity and crystallinity:
Direct solid-state reactions avoid solvent contamination
Nanocrystalline products often obtained without additional crystallization steps
Impurity levels controllable through precursor selection
Cost effectiveness:
Lower equipment costs compared to specialized nanochemistry reactors
Minimal solvent and energy consumption
Direct path from precursors to final product

## Slide 2
Mechanochemical Synthesis of Nanoparticles
Metallic nanoparticles:
Direct milling of bulk metals produces nanocrystalline or amorphous phases
Ball milling of copper, iron, aluminum, or noble metals yields particles 10–100 nm
Applications: catalysis, magnetism, optics, plasmonic sensors
Example: Cu nanoparticles from Cu powder in argon; reactive oxidation controlled by atmosphere
Oxide nanoparticles:
Synthesis from metal salts (oxalates, hydroxides, carbonates) or direct oxidation of metals
High surface area and reactive defects make oxides ideal for catalysis and photocatalysis
TiO₂, ZnO, Fe₂O₃, Al₂O₃ all readily synthesized via mechanochemistry
Example: ZnO nanoparticles from Zn(OH)₂ by 30–60 min planetary milling
Semiconductor quantum dots:
CdS, CdSe, PbS, and other II-VI or IV-VI semiconductors produced as nanocrystals
Particle size determines bandgap and optical properties (size-dependent photoluminescence)
Mechanochemistry offers alternative to wet chemical synthesis
Example: CdSe quantum dots from CdO + SeO₂ with size tuning via milling time
Composition uniformity:
Mechanochemistry inherently mixes phases at atomic scale, producing highly homogeneous nanoparticles
Uniform doping distribution achieved more easily than in thermal methods

## Slide 3
Synthesis of Nanostructures: 1D and 2D
One-dimensional nanostructures (nanofibers, nanowires, nanotubes):
Nanofibers and nanowires:
Metal or oxide nanofibers can be grown by mechanochemical methods combined with templating
Electrospinning followed by mechanochemical densification produces functional nanofibers
Example: SnO₂ nanowires synthesized from SnO₂ precursor via ball milling combined with annealing
Carbon nanotubes (CNTs):
Mechanochemical purification and functionalization of CNTs
Milling opens tubes and creates functional groups (carboxylic acid, hydroxyl, amine)
Enables uniform polymer coating and composite preparation
Two-dimensional nanostructures (nanosheets, nanolayers):
Exfoliation:
Mechanochemical exfoliation of layered materials (graphite, MoS₂, layered hydroxides) produces nanosheets
Ball milling in organic solvents or ionic liquids intercalates species between layers, promoting separation
Example: Graphene from graphite by high-energy ball milling in organic solvent
Nanosheets from synthesis:
Direct formation of ultrathin nanosheets during mechanochemical reactions
Reaction at interfaces naturally produces planar morphologies
Example: Layered double hydroxides (LDH) synthesized as nanosheets via milling of metal hydroxides and carbonate

## Slide 4
Formation Mechanisms
Top-down approach (comminution): Large particles broken into smaller fragments through repeated fracture. Nanoparticles form when fracture size approaches material grain size.
Progressive size reduction follows: or power-law kinetics
Defects accumulate; eventually particles reach a saturation size (10–100 nm typical)
Energy increasingly used for surface area creation rather than new fracture
Bottom-up approach (aggregation): Under certain conditions (high milling intensity, reactive precursors), atoms or small clusters aggregate into nanoparticles.
Nucleation occurs as local concentration exceeds solubility
Diffusion-limited growth builds nanoparticles
Often results in narrower size distribution than pure top-down
Hybrid approaches:
Combine milling of precursors (activating and mixing) with controlled precipitation or solidification
Intermediate grinding steps during synthesis promote nucleation and size control
Example: Wet mechanochemistry—milling in small amounts of solvent enables reaction and precipitation control

## Slide 5
Control of Morphology and Size
Milling parameters affecting nanostructure:
Parameter | Effect on Size/Morphology
Milling time | Longer time → smaller particles, narrower size distribution
Mill speed (RPM) | Higher speed → more energetic collisions, faster size reduction
Ball size and quantity | Larger/more balls → higher energy density, faster reduction
Precursor type | Softer materials (hydroxides) → finer particles; harder oxides → coarser
Atmosphere | Inert → prevents oxidation; air/O₂ → promotes oxidation, may affect size
Temperature | Colder (cryo-mills) → harder particles, sharper fracture; Hot → softer, plastic deformation
Additives and modifiers:
Surfactants/capping agents: Adsorb on nanoparticle surface, prevent agglomeration and growth, stabilize in solution
Polymers: Act as growth inhibitors; enable synthesis of ultrafine particles (<5 nm)
Ionic liquids: Solvent medium that controls nucleation and particle stabilization in wet milling
Multi-stage approaches:
Initial coarse milling produces activated precursor
Fine milling with additives yields narrowly distributed nanoparticles
Post-milling annealing can fuse nanoparticles into desired size/shape

## Slide 6
Current applications:
Catalysis:
Nanoparticles with high surface area and abundant active sites for CO₂ reduction, water splitting, pollutant degradation
Example: TiO₂ nanoparticles for photocatalytic water treatment
Energy storage:
Nanomaterials for battery electrodes and supercapacitors
High surface area enables rapid ion transport and charge storage
Example: LiCoO₂ nanoparticles for lithium-ion batteries
Biomedical:
Metal oxide nanoparticles for drug delivery, imaging, photothermal therapy
Reduced toxicity compared to bulk materials
Example: Fe₃O₄ nanoparticles for magnetic-targeted drug delivery
Electronics and photonics:
Quantum dots for LEDs, displays, solar cells
Plasmonic nanoparticles for sensing and optical applications
Environmental remediation:
Nanoabsorbents for heavy metal removal from water
Photocatalytic nanoparticles for pollutant destruction
Emerging directions:
Integration of mechanochemical synthesis with microfluidics for continuous nanomaterial production
Machine learning to predict and optimize size/morphology from milling parameters
Doping and alloying at the nanoscale during milling
Hybrid mechanochemistry combining with sonication, microwave, or photochemistry