## Slide 1
Differences from Inorganic Mechanochemistry
Organic mechanochemistry presents unique challenges and opportunities compared to inorganic systems:
Molecular vs. ionic bonding: Organic compounds have directional C-C, C-H bonds susceptible to mechanical rupture; often weaker than ionic/metallic bonds
Solubility issues: Many organic products are soluble in solvents, complicating solid-state synthesis; often requires solvent-assisted or liquid-phase grinding
Thermal sensitivity: Organic molecules can decompose at modest temperatures; milling generates local heat requiring temperature control
Polymeric systems: Long-chain molecules respond to mechanical stress through chain scission, entanglement, and reorientation
Reaction pathways: Mechanochemical conditions can activate unusual reaction pathways not accessible thermally, producing novel products
Radical chemistry: Mechanical rupture generates organic radicals, enabling free-radical coupling and functionalization
Key insight: mechanochemistry is particularly valuable for organic synthesis because it avoids traditional solvents and heating, enabling green synthesis of pharmaceuticals and fine chemicals.

## Slide 2
Mechanochemical Synthesis of Organic Compounds
C-C bond formation (coupling reactions):
Grignard-type reactions without reactive metals or solvents
Alkyl halide coupling, aryl coupling (Suzuki-like reactions)
Solid-state synthesis of unsymmetrical biaryls and diaryl compounds
Example: 4-bromobiphenyl from 4-bromobenzene + phenylmagnesium chloride by ball milling
Heterocycle formation:
Synthesis of imidazoles, triazoles, oxazoles from simple precursors without conventional catalysts or solvents
Three-component reactions combining amines, aldehydes, and activated carbon nucleophiles
Mechanochemical protocols reduce synthesis time from hours to minutes
Condensation and functional group transformations:
Amide formation from carboxylic acids and amines
Imine formation from aldehydes and amines
Esterification without acid catalysts
Aldol and Knoevenagel condensations
Advantages:
No or minimal solvent needed
Faster reactions (kinetic enhancement from mechanical activation)
Often higher yields and selectivity compared to solution chemistry
Easier product isolation and purification

## Slide 3
Mechanodegradation of Polymers
Mechanical treatment induces chain scission in polymers, breaking C-C backbone bonds and forming smaller molecular weight fragments and radical end-groups.
Mechanisms:
Random chain scission: Mechanical stress ruptures bonds throughout the polymer
Preferential scission: At weak points, branch points, or heteroatoms
Shear-induced degradation: Flow and friction generate local stresses
Factors affecting degradation rate:
Polymer type (polyethylene, polypropylene, PVC, rubber): different backbone strengths
Milling intensity and time: higher energy → faster degradation
Temperature: elevated T accelerates molecular motion and scission
Atmosphere: oxygen can promote oxidative chain scission; inert atmosphere slows degradation
Additives: plasticizers, stabilizers influence degradation kinetics
Molecular weight evolution:
Viscosity-average molecular weight decreases exponentially with milling time
Polydispersity index (PDI) typically increases (broader molecular weight distribution)
Gel fraction may form from crosslinking via radical recombination
Industrial relevance: Controlled degradation is used to recycle polymers, reduce molecular weight for reprocessing, or produce prepolymers with tailored properties.

## Slide 4
Modification of Polymer Properties
Crystallinity changes:
Mechanical treatment can increase amorphous content (shear-induced disordering) or conversely promote partial crystallization
Altered melting point and glass transition temperature (Tg)
Changes in mechanical properties (stiffness, toughness)
Blend improvement and compatibility:
Co-milling of immiscible polymer blends increases interfacial contact and creates finer, more stable phases
Mechanical energy can enable partial miscibility or in-situ reactive blending
Enhanced mechanical properties compared to simple mechanical mixing
Surface functionalization:
Creating surface defects, radicals, or reactive sites for subsequent chemical grafting
Oxidative surface modification in air atmosphere
Deposition of functional nanoparticles onto polymer surfaces during milling
Nanocomposite formation:
Mechanical treatment disperses nanofillers (clay, carbon nanotubes, graphene) uniformly into polymer matrices
Achieved better dispersion and bonding compared to conventional mixing
Enhanced mechanical, thermal, and electrical properties

## Slide 5
Mechanochemical Polymerization
Solid-state polymerization:
Condensation polymers: polyester, polyamide formation from monomers or oligomers without solvent
Reaction occurs through mechanical activation at surfaces and interfaces
Often requires elevated temperature combined with mechanical treatment
Addition polymerization:
Vinyl monomers or cyclic compounds (lactones, caprolactam) can be polymerized via mechanical initiation
Mechanically generated radicals or ions propagate the chain
Less common than condensation but offers green alternatives to thermal/catalyst initiation
Copolymerization:
Co-milling of different monomers produces random or block copolymers depending on reactivity and conditions
Composition control through stoichiometry of starting monomers
Useful for tailoring copolymer properties without complex chemical synthesis
Examples:
Polyamide (nylon) from diamine + dicarboxylic acid by ball milling
Polyester from diol + diacid in solid state
Poly(methyl methacrylate) from monomer with mechanically-generated peroxide initiator

## Slide 6
Industrial and Practical Applications
Pharmaceutical industry:
Mechanochemical synthesis of active pharmaceutical ingredients (APIs) reduces production cost and waste
Solid-state synthesis enables scaling without expensive equipment
Examples: aspirin, paracetamol, and novel drug candidates synthesized mechanochemically
Polymer recycling and upcycling:
Mechanical degradation of post-consumer plastic waste produces shorter-chain oligomers suitable for repolymerization
Chemical recycling: degraded polymers converted to monomers via mechanochemical routes combined with other methods
Materials science:
Polymer nanocomposites with superior properties
Controlled copolymer architectures
Novel polymer blends with enhanced compatibility
Green chemistry credentials:
Solvent-free or minimal solvent processes
Room-temperature or low-temperature synthesis
Reduced waste, improved atom economy
Energy-efficient compared to conventional industrial routes