## Slide 1
Environmental Aspects of Mechanochemistry
Mechanochemistry and Green Chemistry
The 12 Principles of Green Chemistry, established by Anastas and Warner, provide a framework for sustainable chemical processes. Mechanochemistry aligns well with many of these principles.
Relevant green chemistry principles:
1. Prevention: Avoid waste generation by designing synthesis for 100% atom economy 2. Atom economy: Minimize waste by using all reactants; no excess reagents needed in solid-state reactions 5. Safer solvents: Eliminate or minimize solvent use entirely; ideal for mechanochemistry 6. Energy efficiency: Lower temperature and pressure requirements reduce energy footprint 8. Reduce derivatives: Direct synthesis without protecting group chemistry 10. Reduce toxicity: Inherently safer reactions; no toxic solvents or byproducts
Mechanochemistry alignment:
Solvent-free or minimal-solvent processes naturally avoid toxic organic solvents
Room-temperature operation reduces energy input
Direct synthesis reduces process complexity and waste
Scalable from lab to production maintaining green characteristics

## Slide 2
Environmental Aspects of Mechanochemistry
Environmental Advantages of Mechanochemical Processes
Solvent elimination:
Traditional synthesis: reactions conducted in organic solvents (toluene, dichloromethane, acetone, DMF) requiring distillation, waste treatment, incineration.
Mechanochemical alternative: solid-state or solvent-free reactions eliminate solvent recovery and disposal costs, ~50–90% reduction in chemical waste per kg product.
Example: synthesis of aspirin from acetic anhydride and salicylic acid
Conventional: solvent-based, ~100 L solvent per kg aspirin
Mechanochemical: dry milling, solvent-free
Energy efficiency:
Conventional thermal synthesis: often requires 120–200°C or higher; energy-intensive heating, cooling cycles Mechanochemical synthesis: often room temperature or <100°C; minimal energy per reaction
Energy comparison: ball milling typically consumes 5–20 kWh/kg vs. 50–100+ kWh/kg for thermal processes
Reaction time and yield:
Mechanochemistry: minutes to hours for complete conversion Conventional: hours to days
Higher atom economy: fewer side reactions, higher yields (often 90–98% vs. 70–85%)
Water consumption:
Mechanochemistry: minimal or zero water in reaction (dry grinding) Conventional wet chemistry: significant water use for solvation, washing, crystallization

## Slide 3
Environmental Aspects of Mechanochemistry
Designing Green Mechanochemical Processes
Precursor selection:
Choose starting materials with minimal environmental impact:
Prefer oxides, carbonates, or hydroxides over toxic metal salts
Select bio-based or renewable precursors where possible
Minimize heavy metal content (Pb, Cd, Cr forbidden in many applications)
Example: synthesis of MgAl₂O₄ spinel
Green route: MgO + Al₂O₃ (simple oxides, industrially available, low toxicity)
Conventional: Mg(NO₃)₂ + Al(NO₃)₃ (toxic nitrogen oxides released upon decomposition)
Milling atmosphere and media:
Inert atmosphere (argon, nitrogen): prevents oxidation and contamination
Air or oxygen atmosphere: enables on-purpose oxidation without oxidizing agents
Grinding media: ceramic, agate, or tungsten carbide preferred over steel (lower contamination)
Minimizing additives:
Dry milling preferred over liquid-assisted milling (LAG) to avoid solvent disposal
If LAG needed, use water or biodegradable solvents (ethanol, glycerol)
Milling auxiliary agents: kept to minimum necessary (surfactants, grinding aids)
Post-treatment optimization:
Direct product use preferred
If heating required, combine with electrical or solar energy
Minimal washing; if necessary, use water only

## Slide 4
Environmental Aspects of Mechanochemistry
Life Cycle Assessment (LCA) of Mechanochemical Synthesis
LCA methodology:
Quantitative environmental impact evaluation from raw materials to disposal.
Four phases:
Goal and scope definition: System boundaries, functional unit (e.g., 1 kg product)
Life cycle inventory (LCI): Account for all inputs (materials, energy, water) and outputs (products, emissions, waste)
Life cycle impact assessment (LCIA): Evaluate environmental impacts (climate change, water use, toxicity, energy)
Interpretation: Compare scenarios, identify improvement opportunities
Example comparison: TiO₂ nanoparticles
Metric | Sol-gel (conventional) | Mechanochemical
Raw materials | TiCl₄, ethanol, water | TiO₂, ethanol (optional)
Energy (kWh/kg) | 80 | 15
Solvent waste (L/kg) | 50 | 0–5
CO₂ emissions (kg/kg) | 25 | 4
Water consumption (L/kg) | 100 | 5
Product purity | 99.5% | 99.8%
Cost ($/kg) | 800 | 200
Mechanochemical route shows 80–90% reduction in environmental impact across most metrics.
Case study: LaFeO₃ perovskite Conventional synthesis (solution combustion at 600°C) vs. mechanochemical (room-temperature ball milling)
Energy: 70 kWh → 8 kWh (88% reduction)
Waste: significant organic residues → minimal inorganic dust
LCA score: mechanochemical 60% lower environmental burden

## Slide 5
Environmental Aspects of Mechanochemistry
Waste Recycling and Remediation via Mechanochemistry
Battery recycling:
Lithium-ion batteries contain valuable metals (Li, Co, Ni) and toxic lead or cadmium. Mechanical treatment (crushing, grinding) combined with leaching recovers metals.
Dry milling: separates cathode material, anode graphite, separator
Acid leaching of milled cathode: dissolves Co, Ni, Li
Recovery rates: 90–98% of strategic metals
Alternative to pyrometallurgy (high-temperature energy-intensive smelting)
Plastic waste recycling:
Mechanical degradation (grinding) of plastic waste produces shorter-chain oligomers suitable for repolymerization or use as monomers.
PET (polyethylene terephthalate) from bottles mechanically depolymerized via grinding and thermal treatment
Energy: 50% lower than virgin synthesis
Example: Adidas and other brands now use mechanochemically recycled polyester in products
Heavy metal remediation:
Contaminated soil or waste water treated by mechanochemically activated adsorbents (activated carbon, clay, oxides).
Milling increases surface area and reactive sites
Adsorption capacity 2–5× higher than untreated material
Cost reduction and efficiency improvement
Hazardous waste destruction:
Persistent organic pollutants (POPs) and dioxins mechanochemically activated for destruction.
Ball milling can break C-Cl bonds and aromatic rings
Combined with oxidizing atmosphere enables complete mineralization to CO₂ and HCl
Non-toxic waste product

## Slide 6
Environmental Aspects of Mechanochemistry
Sustainability Strategy and Future Outlook
Current status:
Mechanochemistry increasingly recognized as key green technology for circular economy and carbon-neutral manufacturing.
Publications trend: Mechanochemistry journals and conference abstracts emphasize sustainability; >40% of recent papers mention green chemistry, LCA, or waste reduction.
Industrial adoption:
Pharmaceutical: several APIs synthesized mechanochemically at multi-ton scales (Merck, Novartis pilot programs)
Cement/concrete: mechanical activation now standard in modern plants
Recycling: mechanochemical preprocessing increasingly common in e-waste and battery recycling
Policy drivers:
EU Green Deal: targets circular economy and CO₂ neutrality by 2050
China and other nations implementing strict waste management and emissions regulations
Corporate sustainability commitments (net-zero targets) driving mechanochemical investment
Future perspectives:
Integration of mechanochemistry with renewable energy (solar, wind) to power mills
Coupling with other green technologies (enzymatic catalysis, photochemistry)
AI-optimized process design for minimal environmental footprint
Standardization of LCA methodology for mechanochemical processes
Scale-up of waste recycling processes to industrial production levels
Challenges:
Upfront capital cost for equipment
Knowledge gap in industry; education and training needed
Standardization and regulatory approval for new processes
Competition with cheaper (but less sustainable) conventional methods
Takeaway: Mechanochemistry is not just scientifically interesting—it is a practical pathway to sustainable manufacturing aligned with global environmental and economic imperatives