## Slide 1: Corrosion and passivation
Fyodor Malchik

## Slide 2: Metal Corrosion
“the destruction of a material by chemical or electrochemical reaction to its environment”
typically a transfer of electrons from one metal to another through an Oxidation-Reduction Reaction.

## Slide 3: Oxidation - Reduction Reduction
Anodic metal gives up electrons (oxidation)
Cathodic metal accepts electrons (reduction)
Or gases accept electrons (reduction)

## Slide 4: Corrosion Mechanism
Cathodic cell
  discussion of emf
galvanic series
intergranular corrosion
oxidation-reduction of iron
salt effects
Notes: electrochemical corrosion requires
  2 dissimilar metals (anode and cathode)
  electrolyte (solution that can support the flow of electrons)
  conductor (metallic pathway for electrons to flow between metals)
  potential is measured in emf series
galvanic series is practical listing of emf potentials in less idealized conditions
intergranular corrosion at boundaries, different potential for different structures e.g. pearlite is part carbide and part alpha iron
oxidation reduction of iron
salt draw moisture to the surface, chlorides react with rust making is flake off faster and exposing more iron for the oxidation reaction

## Slide 5: Slides on Impact of Corrosion
Aluminum corrosion
Pitting
Crevice corrosion
Contaminants
Environments
Notes: Aluminum - Steel corrosion is a galvanic reaction
Pitting - isolated breakdown of coating system, break in film is anode and the rest is a cathode (oxidation concentration cell)
example of pitting of a bridge flange
Crevice Corrosion is caused by the formation of an oxidation concentration cell.
contaminants in the air accelerate corrosion, sulfur and acid rain participate in reactions
Steel Structure Painting Council (oil base life prediction for coatings)

## Slide 6: Basics of Corrosion
EMF series is a numeric rating of potential under ideal conditions
Galvanic Series is a practical listing
Galvanic Protection

## Slide 9: Steel Corrosion
Initial Oxidation Reaction
Secondary Oxidation Reaction
Rust

## Slide 11: Corrosion potential calculation
Reduction Reaction must have higher potential than the oxidation reaction or they will not form a cathodic cell
-0.440 V
-0.763 V
Relative measure of corrosion

## Slide 12: Acceleration of Corrosion
Physical Characteristics
  exposed area (less, increases corrosion rate)
  time of exposure (more time, more corrosion)
Environmental Characteristics
  acidic environment
  sulfur gas environment
  temperature (high temps, more corrosion)
  moisture (oxygenated moisture)

## Slide 13: Passivation
A protective film in oxidizing atmospheres
  chromium,nickel, titanium, aluminum
Metal oxide layer adheres to parent metal
  barrier against further damage
  self-healing if scratched
Sensitive to environmental conditions
  passivated metal may have high corrosion rates

## Slide 14: Forms of Corrosion
Uniform corrosion of a single metal
  usually an electrochemical reaction at granular level
  relatively slow and predictable
  rusting of exposed steel, tarnished silver
  easily corrected with coatings and regular maintenance

## Slide 15: Forms of Corrosion
Galvanic Corrosion
  2 dissimilar metals, electrolyte, electrical connection and oxygen
Pitting Corrosion
  Localized corrosion forming holes or indentations
  Difficult to initially detect

## Slide 16: Forms of Corrosion
Crevice Corrosion
  narrow crevice filled with ionized solution
  Oxygen-rich on the outside, oxygen-poor on the inside
  metals oxidize with salt anions FeCl2 and pH rises in cathodic zone
  H+ may destroy passivity

## Slide 17: Forms of Corrosion
Intergranular Corrosion
  corrosion along grain boundaries at microscopic level
  stainless steels and heat treated high-strength steels
  carbides precipitate along grain boundaries leaving these areas with no alloyed Chromium
  Welds can have this same depletion effect

## Slide 18: Forms of Corrosion
Cavitation and Erosion in Pipe
  particulate matter
  turbulent flow
  abrades away the corrosion product
  abrasion of zinc coatings

## Slide 19: Forms of Corrosion
Stress Corrosion Cracking
  tensile stress and corrosive environments
  cracks are initiated at corrosion areas
  tensile stresses propagate the crack
  corrosion further deteriorate crack
  etc.....

## Slide 20: Reinforcement Corrosion

## Slide 21: Corrosion Products
Fe + 2OH = Fe(OH)2
Oxidation of Fe(OH)2
Fe(OH)3 (rust)
Passivity barrier breaks down
Presence of Oxygen
Moisture

## Slide 22: Corrosion of Metals in Concrete Reinforcing Steel & Prestressing Steel
Concrete is Normally Highly Alkaline
  Protects Steel from Rusting if Properly Embedded
If Corrosion Occurs, the Reaction Products are Greater in Volume Than the Original Steel
Corrosion Initiation and Rate Depends On
  Amount of Concrete Cover, Quality of Concrete
  Details of Construction, & Exposure to Chlorides

## Slide 24: Avoiding Corrosive Situations
Choose couple metals close on the galvanic series
Use large anode, and small cathode areas
Electrically insulate dissimilar metals
Connect a more anodic metal to the system
Avoid turbulent flow and impingements in pipe systems

## Slide 25: Examples of Corrosion in CE
Steel strapping or iron nails with copper pipe is ok, but they may rust with time.
Never use Copper strapping or attachments with steel pipe, steel pipe will corrode
condensation on the bottom of cold water pipe

## Slide 26: Corrosion Prevention
Coatings
  Barrier films
  Inhibitive Pigments
  Sacrificial treatments
  Paint
Active Cathodic Protection